|  | KJF208 |
| --- | --- |
|  | Salt Proof Air Filter Testing Method 測試方法 Dot Spot Efficiency (in NBS Testing Method) 比色法 Arrestance (in AFI Testing Method) 比重法 MERV 90~95% > 99% 14 By ASHRAE Standard 52.1-1992 (Equal to EN 779) 依ASHRAE 52.1-1992標準 (德國EN 779) By ASHRAE 52.2-1999 Standard 依ASHRAE 52.2-1999標準 防鹽害空氣濾網 Usage: Buildings, Hotels, Resort Centers. Factories located along the beach. Nuclear Power Plants, Heat Power Plant to prevent electrical insulation due to corrosion. Semiconductor plants to eliminate sodium to have any adverse effects on products. Process of Precision machinery to decrease defective products happen and eliminate the impaction of raw materials proportion. Features: Salt Proof Air Filters are specially designed for the environment like factories, buildings which are located along the beach, Nuclear Power Plants and etc. Most of particle size of salt is poly-dispersed and in the range of 0.5μm to 30μm. AIRREX Salt-Proof Air Filter provides a 95% high efficiency in salt holding capacity. The salt will not spray again or hydrolyze by moisture when it is caught by the filter. Construction: The particle size of salt is in a range of 0.5μm to 30μm. The filter media contains two layers of fiberglass materials in different densities. The rough layer can catch the larger particle size in order to reduce the |

KJF 208

load of dense media and extends filter’s life span. Media: The filter media is contained two layers of glass microfiber in different densities. Media is with excellent water repellency, and provides 95% high efficiency in salt holding capacity (per ASHRAE 52.1-1992 standard, in NBS Test Method). Both edges of aluminum separators are rolled to prevent media tearing and provide maximum integrity. Outer Frame: The frame is available for Wooden and Metal Frame (Galvanized Steel, Aluminum and Stainless Steel) in box type or header type. 特色：適用於沿海地區工廠、大樓等，處於含有高濃度鹽份的空氣中，海鹽粒子之粒徑為多分散型，粒徑 分佈從0.5um至30um，海鹽粒子對金屬造成腐蝕生銹，使產品品質不良，防鹽害濾網即針對此種環 境用途而特別設計之空氣過濾網。 效率：依ASHRAE 52.1-1992標準法測試，濾網具比色法效率95%效率之捕集能力，被濾網捕捉之海鹽粒子，經溼氣潮解溶化後，亦不會再度飛散。 濾材：濾材以粗、密二層玻璃纖維濾材重疊組成，較粗之海鹽粒子由粗濾材捕集以減低密濾材之負擔，以延長使用時間，濾材具有良好之撥水性，被捕集之海鹽粒子不受潮解而有飛散的特性。 外框：框材可選用木框、鍍鋅鐵框、鋁框或不銹鋼框。

KJF 208

Performance Data - Salt Proof Air Filter 中效率濾網性能表 - 防鹽害空氣濾網空氣濾網 Efficiency Nominal Size Actual Size Rated Capacity Pressure Drop 效率 通稱尺寸 實際尺寸 額定風量 壓力損失 （％） （W*H*D） （W*H*D） （CMH） （Pa） Dot Spot Efficiency (in NBS) 比色法 Arrestance (in AFI) 比重法 （inch） （mm） Initial Resistance 初壓損 Final Resistance 末壓損 Standard Capacity 標準風量 95 ＞ 99 12*24*6 305*610*150 850 117 300 24*24*6 610*610*150 1700 12*24*12 305*610*292 1700 167 350 24*24*12 610*610*292 3400 High Capacity 高風量 95 ＞ 99 12*24*12 305*610*292 2125 174 350 24*24*12 610*610*292 4250 *Special Sizes are available upon request. ※特殊規格可生產製造

KJF 208

Material and Service Conditions 材質和使用條件 Type 型式 Description 說明 Construction 總成 Media 濾材 Ultra-Fine Glass Fiber 超細玻璃纖維濾紙 Support Grid 支撐材 Corrugated Aluminum Separators 波浪隔板 Sealant 密封膠 PU Base Gasket Material 墊片材質 Neoprene Rubber 新平橡膠 Frame Material 外框材質 Wooden Frame 木框 Metal Frame 金屬框 Frame Type 外框型式 Box Type 箱型 Single Header 單法蘭 Service Conditions 使用條件 The maximum continuous use temperature 連續使用最高溫度 ℃ 60 Instant Highest Humidity 使用瞬間最高濕度 % RH 100 (No condensation state) 100（無結露狀態下） 名 稱:康智富科技有限公司 統 編:29168436 地 址:新北市永和區仁愛路141巷30弄26號1樓 電 話:+886-2-29256286 傳 真:+886-2-29256096 E-MAIL :ks.best@msa.hinet.net