|  | KJF209 |
| --- | --- |
|  | Compressor Filter 空壓機濾網 Testing Method 測試方法 Particle Size 粒徑 Efficiency (%) 效率 10 98% 2 99.97% By ASHRAE 52.1-1992 Standard (Equal to EN 779） 依ASHRAE52.1-1992標準(德國EN 779) |

KJF209

Features: Heavy duty construction provides additional collapse strength and security. Increased extra 20% filtering area for lower pressure drop. 94% ASHRAE Dust Spot efficiency to provide additional protection for high speed rotating equipment. Excellent clean ability. Panel to be cleanable by compressed air or washable by mild detergent. Media pack can remain fine shape and space. Greater dust collection capacity. Withstands differential high pressure and prevents contaminant bypass. 特色：【前段】維修、安裝容易，集塵能力佳。 【後段】低壓損過濾面積超過20%，提高高速運轉機械機械的保護作用。 效率：【前段】濾網依ASHRAE 52.1-1992標準法測試，濾網具比色法效率98%通過10um。 【後段】濾網效率99.97%通過2um。 濾材：【前段】可選用木漿纖維或多元聚酯熱熔棉。 【後段】是由超細玻璃纖維所製，濾網頂端及底部以PU膠密封，外框與濾材無洩漏之虞。 外框：框材可選用鍍鋅鐵框或不銹鋼框。

KJF209

Performance Data - Compressor Filter 中效率濾網性能表 - 空壓機濾網 Efficiency Particle Size Nominal Size Actual Size Rated Capacity Pressure Drop 效率 粒徑 通稱尺寸 實際尺寸 額定風量 壓力損失 （W*H*D） （W*H*D） （Pa） （％） （um） （inch） （mm） （CMH） Initial Resistance 初壓損 Final Resistance 末壓損 Pre-Filter – Wood Pulp Fiber Fine Filter (HEPA) – Deep Pleat Type 前段-木漿纖維、後段-隔版型 98 10 24*24*1-1/2 595*595*38 3400 116 250 99.97 2 24*24*11-1/2 595*595*292 3400 195 500 Pre-Filter – Polyester Fine Filter (HEPA) – V Type 前段-多元聚酯熱熔棉、後段-V型 98 10 24*24*1-1/2 595*595*38 3400 82 250 99.97 2 24*24*11-1/2 595*595*292 3400 120 500 *Special Sizes are available upon request. ※特殊規格可生產製造。 Material and Service Conditions 材質和使用條件 Type 型式 Description 說明 Construction 總成 Category 類別 Pre-Filter 前段 Fine Filter (HEPA) 後段 Type 型式 Corrugated Aluminum Separators 浪型 Deep Pleat Type 隔板型 V Type V型 Media 濾材 Wood Pulp Fiber 木漿纖維 Polyester 多元聚酯熱熔棉 Glass Fiber 玻璃纖維 Support Grid 支撐材 - Corrugated Aluminum Separators 波浪隔板 Hot Melt Adhesive 熱熔膠

KJF209

Material and Service Conditions 材質和使用條件 Construction 總成 Sealant 密封膠 - Epoxy Resin 環氧樹脂 Gasket Material 墊片材質 - Neoprene Rubber 新平橡膠 Gasket Location 墊片位置 - Both sides of filter 雙面 Frame Material 外框材質 Galvanized Steel 鍍鋅鐵框 Galvanized Steel 鍍鋅鐵框 Upstream Face Guard 上風處護網 4*4 Galvanized Metal 4*4鍍鋅鐵網 - Downstream Face Guard 下風處護網 1/2” Expanded Galvanized Metal 1/2” 擴張鐵網 1/2” Expanded Galvanized Metal 1/2” 擴張鐵網 Brace 拉條 Upstream 上風處 Option Service Conditions 使用條件 The maximum continuous use temperature 連續使用最高溫度 ℃ 60 Instant Highest Humidity 使用瞬間最高濕度 % RH 100 (No condensation state) 100（無結露狀態下） 名 稱:康智富科技有限公司 統 編:29168436 地 址:新北市永和區仁愛路141巷30弄26號1樓 電 話:+886-2-29256286 傳 真:+886-2-29256096 E-MAIL :ks.best@msa.hinet.net

# Text boxes

Pre-Filter Filter.

Specifications:

Size:					24”X24”X1-1/2”

Filter Media: 			Synthetic Fiber

Filter Efficiency: 		98% on 10 micron particle size or higher

Frame: 				Galvanized Steel

Sealant:: 	Filter media pack to be encapsulated top and bottom with PVC adhesive.

Screen: 				4x4 Galvanized Metal on upstream face

1/2” Expanded Metal on downstream face

Removal Strap: 			Upstream face

Nominal Rated Capacity:	2500 CFM

Features:

- Excellent clean ability.  Panel to be cleanable by compressed air or washable by mild detergent , . Media pack can remain fine shape and space.

- Ease of maintenance and installation.

- Lower pressure drop, greater dust collection capacity.

- Withstands differential high pressure and prevents contaminant bypass.

Fine Filter (HEPA)

Specifications:

Size:					24”X24”X11-1/2”

Filter Media:			Water-resistant Glass Microfiber

Filter Efficiency:			99.97% on 2.0 micron particle size (94% ASHRAE Dust Spot)

Frame:					12mm Galvanized Steel

Sealant:	Filter media pack to be encapsulated top and bottom with epoxy adhesive.

Gasket:	HEPA rated.  Gasket seals in frame on downstream or two faces.

Corner Glides:				P.V.C. angle on bottom corners.

Fin Spacers:				Corrugated Aluminum

ASHRAE Capacity:		585 grams at 4” WG (Independently Tested)

Collapse Strength:			Greater than 34” WG (Independently Tested)

Removal Strap:			Pull strap across panel face, easily remove.

Nominal Rated Capacity:	2500 CFM